## Slide 1
M-65 grade concrete
A1 values corresponds to 67.5 MPa concrete
A2 values corresponds to 77.5 MPa concrete
A3 values corresponds to 87.5 MPa concrete
M-70 grade concrete

## Slide 2
M-75 grade concrete
M-80 grade concrete

## Slide 3
M-85 grade concrete
M-90 grade concrete

## Slide 4
A1=67.5 MPa concrete
A2= 77.5 MPa concrete
A3=87.5 MPa concrete
Chart: Mean deviations comparision
| 65 | 70 | 75 | 80 | 85 | 90
IS-456:2000 | 1.0266 | 1.0672 | 1.1184 | 1.1514 | 1.2035 | 1.2518
A1 | 0.97544 | 1.0156 | 1.0632 | 1.094 | 1.1426 | 1.1875
A2 | 0.89719 | 0.93672 | 0.97835 | 1.0053 | 1.0487 | 1.0885
A3 | 0.85048 | 0.88751 | 0.92609 | 0.95108 | 0.99017 | 1.0268
IRC 112 | 0.99983 | 0.99328 | 1.0008 | 0.98601 | 0.99315 | 1.0046

## Slide 5
Grade of concrete | IS 456 | A1 | A2 | A3 | IRC 112
65 | 1.103 | 0.973 | 0.847 | 0.803 | 1.000
70 | 1.067 | 1.016 | 0.937 | 0.888 | 0.993
75 | 1.118 | 1.063 | 0.978 | 0.926 | 1.001
80 | 1.151 | 1.094 | 1.005 | 0.951 | 0.986
85 | 1.204 | 1.143 | 1.049 | 0.990 | 0.993
90 | 1.252 | 1.188 | 1.089 | 1.027 | 1.005

## Slide 6
Chart: Mean deviations of 67.5 MPa
| 65 | 70
 | 0.97544 | 1.0156

## Slide 7
Chart: Mean deviations of 77.5 MPa
| 75 | 80
 | 0.97835 | 1.0053

## Slide 8
Chart: Mean deviations of 87.5 MPa
| 85 | 90
 | 0.99017 | 1.0268